# Supplementary Material for

Surface-Functionalized ZnO Nanorods via PEG-Assisted Stabilization for Durable Antibacterial Lyocell Fibers

Biao Liu1, Xin Wei1, Zexin Lin1, Peiyu Cui1, Junlong Yao1, Xiaobo Ye2, Bin Fang2, 
Yani Guo1,* and Yimin Sun1,*

1Hubei Key Laboratory of Plasma Chemistry and Advanced Materials, School of Materials Science and Engineering, Wuhan Institute of Technology, Wuhan, China

2Dangyang Hongyang New Material Technology Co., Ltd., Dangyang, China

*Corresponding Authors: Yani Guo. Email: guoyni@163.com; Yimin Sun. Email: ymsun@wit.edu.cn

Fig. S1: SEM images of ZnO/Lyocell composite fibers with 3 wt% ZnO loading prepared (A-C) with PEG and (D-F) without PEG

Fig. S2: SEM images of Lyocell fibers with different ZnO concentrations: (A) /Lyocell; (B) 1%-ZnO/Lyocell; (C) 2%-ZnO/Lyocell; (D) 3%-ZnO/Lyocell; (E) 4%-ZnO/Lyocell; (F) 5%-ZnO/Lyocell.

Fig. S3: Antibacterial performance of ZnO/Lyocell composite fibers: (A, B) under dark conditions, (C, D) at 30% and 80% relative humidity (T-3); (A, C) colony counting images, (B, D) corresponding antibacterial efficiency.

Fig. S3A shows the antibacterial performance of ZnO/Lyocell composite fibers against E. coli and S. aureus under dark conditions evaluated by the colony counting method, with pristine Lyocell fibers used as the control. The corresponding antibacterial efficiency is summarized in Fig. S3B. The results indicate that the composite fibers still exhibit moderate antibacterial activity in the absence of light. However, the antibacterial efficiency is substantially lower than that obtained under fixed light irradiation. Specifically, the antibacterial rates of T-5 fibers against both bacterial strains are approximately 60% under dark conditions, whereas values exceeding 98% are achieved under light irradiation. This pronounced difference can be attributed to the suppressed generation of reactive oxygen species (ROS) in the absence of light, which weakens the photocatalytic bactericidal activity of ZnO. Figures S3C and S3D present the antibacterial performance of T-3 composite fibers under different relative humidity (RH) conditions. At 30% RH, the antibacterial rates reach 88% for E. coli and 92% for S. aureus, while the corresponding values at 89% RH are 82% and 93%, respectively. No significant variation in antibacterial efficiency is observed with increasing humidity, indicating that the antibacterial performance of the composite fibers is relatively insensitive to environmental humidity within the tested range.

Fig. S4: Photos of inhibition zones against E. coli (A) and S. aureus (B).

Table S1. The tensile strength and elongation at break of Lyocell fibers with different ZnO contents

| ZnO content (wt%) | 0 | 1 | 2 | 3 | 4 | 5 |
| --- | --- | --- | --- | --- | --- | --- |
| Tensile strength (Mpa) | 260 | 221 | 196 | 184 | 180 | 138 |
| Tensile elongation at break (%) | 5.61 | 2.79 | 1.95 | 1.62 | 1.41 | 1.22 |

Table S2. Comparison of antibacterial performance of cellulose-based fibers modified with inorganic antimicrobial agents reported in recent literature.

| Sample | Antibacterial performance (%) | Reference |
| --- | --- | --- |
| Rod-like ZnO /Lyocell composite fiber | T-3: 96 (E. coli), 95 (S. aureus) T-5: 98 (E. coli and S. aureus) | this work |
| ZnO-modified Lyocell fabric | 80 (E. coli), 97 (S. aureus) | [1] |
| ZnO-coated cotton fiber | 50 (E. coli), 49 (S. aureus) | [2] |
| Ag nanoparticles-modified cotton fiber | 94(E. coli), 98 (S. aureus) | [3] |
| Cu ion-modified Lyocell fiber | 99 (E. coli), 98 (S. aureus) | [4] |
| Cu/Zn galvanic coated cotton | 97 (E. coli), 98 (S. aureus) | [5] |

Note: Antibacterial efficiencies were extracted from the respective references and measured under different experimental conditions. The comparison is intended to provide a general performance benchmark rather than a strict one-to-one evaluation.

[1]. Wang X, Wang S, Li Y, Jin X, Dong C. Preparation and properties of low fibrillated antibacterial Lyocell fiber. Arab J Chem. 2024;17(4): 105658. doi:10.1016/j.arabjc.2024.105658.

[2]. El-Nahhal IM, Salem J, Anbar R, Kodeh  FS,  Elmanama A. Preparation and antimicrobial activity of ZnO-NPs coated cotton/starch and their functionalized ZnO-Ag/cotton and Zn (II) curcumin/cotton materials. Scientific reports, 2020;10(1): 5410. doi:10.1038/s41598-020-61306-6.

[3]. Zhang S, Zhang T, He J, Dong X. Effect of AgNP distribution on the cotton fiber on the durability of antibacterial cotton fabrics. Cellulose. 2021;28:9489–9504. doi:10.1007/s10570-021-04113-0.

[4]. Wendler F, Schulze T, Bauer J, Redlingshöfer B. Bioactive lyocell fibers with inherent antibacterial, antiviral and antifungal properties. Molecules, 2024;29(9): 2054. doi:10.3390/molecules29092054.

[5]. Zhang S, Dong H, He R, Wang N, Zhao Q, Yang L, et al. Hydro electroactive Cu/Zn coated cotton fiber nonwovens for antibacterial and antiviral applications. Int J Biol Macromol. 2022;207:100-109. doi: 10.1016/j.ijbiomac.2022.02.155.