Supporting Information

p-Phenylenediamine-benzoquinone polymer/reduced graphene oxide flexible composite films as a cathode material for rechargeable lithium-ion batteries

Zhouqishuo Cai, Donghua Liu, Yanan Zhao, Zewen Lin, Shumin Lin, Dan Zhong, Hua Bai*

College of Materials, Xiamen University, Xiamen 361005, P R China

E-mail addresses: baihua@xmu.edu.cn

Scheme S1 Proposed polymerization mechanism of PPD-BQ.

Figure S1 Optical photographs of (a) PPD-BQ-1, (b) PPD-BQ-2, (c) PPD-BQ-3, (d) PPD-BQ-5, and (e) PPD-BQ-10.

Scheme S2. Proposed charge–discharge mechanism of PPD-BQ in lithium-ion batteries.

Figure S2 Fig. S2(a) presents low-magnification SEM images (scale bar: 10 μm) of PPD-BQ-1, PPD-BQ-2, PPD-BQ-3, PPD-BQ-5, and PPD-BQ-10, clearly showing the overall morphology and extensive agglomeration of polymer particles across all samples. Fig. S2(b) provides corresponding high-magnification SEM images (scale bar: 2 μm), which further reveal the dense and irregular surfaces of the aggregated particles, indicating limited porosity and restricted accessibility of electrolyte to the internal redox-active sites.

Figure S3 UV-vis spectra of PPD standard solutions at different concentrations (a), and electrolyte solutions after immersing PPD-BQ-1 (b) and PPD-BQ/RGO (c) for various periods.

UV-vis spectroscopy were performed on the electrolyte solutions after immersing PPD-BQ-1 and PPD-BQ/RGO films for different periods (1, 5, 10, 14, and 30 days). The characteristic absorption bands of p-phenylenediamine around 265 and 300 nm were monitored to track the dissolution of the polymer or composite films. As shown in Figure S3, the absorbance at these bands increases progressively with immersion time for PPD-BQ-1, indicating continuous dissolution of the polymer into the electrolyte. In contrast, for PPD-BQ/RGO composite films, only slightly changes in absorbance are observed over the same period, confirming that the RGO framework effectively suppresses polymer dissolution through strong interfacial interactions. These results are consistent with the visual observation in Figure 3h and provide quantitative evidence for the enhanced cycling stability of the composite films.

Table S1 Synthesis conditions and corresponding sample names of PPD-BQ/RGO composite films

| Names of products | a | b | c | T | t |
| --- | --- | --- | --- | --- | --- |
| PPD-BQ/RGO-A-1 | 30 | 30 | 5 | 50 | 24 |
| PPD-BQ/RGO-A-2 | 30 | 30 | 5 | 50 | 24 |
| PPD-BQ/RGO-A-3 | 30 | 30 | 3 | 50 | 24 |
| PPD-BQ/RGO-A-4 | 30 | 30 | 1 | 50 | 24 |
| PPD-BQ/RGO-A-5 | 30 | 30 | 0.2 | 50 | 24 |
| PPD-BQ/RGO-A-6 | 30 | 30 | 0 | 50 | 24 |
| PPD-BQ/RGO-B-1 | 30 | 30 | 5 | 50 | 24 |
| PPD-BQ/RGO-B-2 | 20 | 40 | 5 | 50 | 24 |
| PPD-BQ/RGO-B-3 | 10 | 50 | 5 | 50 | 24 |
| PPD-BQ/RGO-B-4 | 20 | 20 | 5 | 50 | 24 |
| PPD-BQ/RGO-B-5 | 40 | 40 | 5 | 50 | 24 |
| PPD-BQ/RGO-B-6 | 10 | 10 | 5 | 50 | 24 |
| PPD-BQ/RGO-C-1 | 20 | 20 | 5 | 50 | 24 |
| PPD-BQ/RGO-C-2 | 20 | 20 | 5 | 65 | 24 |
| PPD-BQ/RGO-C-3 | 20 | 20 | 5 | 90 | 24 |
| PPD-BQ/RGO-D-1 | 20 | 20 | 5 | 50 | 24 |
| PPD-BQ/RGO-D-2 | 20 | 20 | 5 | 50 | 18 |
| PPD-BQ/RGO-D-3 | 20 | 20 | 5 | 50 | 12 |
| PPD-BQ/RGO-D-4 | 20 | 20 | 5 | 50 | 48 |

Figure S4 Effects of synthesis conditions on the electrochemical performance of PPD-BQ/RGO composite films: (a) pH, (b) feed ratio of PPD/BQ/GO, (c) reaction temperature, and (d) reaction time.

As shown in Figure S4a, comparison between PPD-BQ/RGO-A-1 and PPD-BQ/RGO-A-2 indicates that the reaction proceeded more efficiently in air than under an argon atmosphere. This can be attributed to the polymerization mechanism illustrated in Figure S1. During the 1,4-addition reaction between PPD and BQ, the quinone groups are reduced to phenolic structures. Subsequent polymerization requires the reoxidation of these phenolic intermediates back to quinone structures. Oxygen in air may facilitate this oxidation process, thereby promoting continuous polymerization. In addition, comparison among PPD-BQ/RGO-A-2, -3, -4, -5, and -6 shows that increasing the pH of the reaction system by decreasing the amount of hydrochloric acid leads to higher initial discharge capacities but poorer cycling stability. This phenomenon suggests that more low-molecular-weight species are adsorbed onto the RGO nanosheets under weakly acidic or neutral conditions, and these species are more likely to detach during cycling, resulting in accelerated capacity decay. In contrast, acidic conditions are more favorable for the in situ polymerization process. Notably, composite films could not be successfully formed under alkaline conditions, and therefore, their electrochemical performance was not evaluated. Based on these results, the synthesis conditions used for PPD-BQ/RGO-A-2 were selected as optimal.

As shown in Figure S4b, comparison among PPD-BQ/RGO-B-1, -2, and -3 indicates that the composite films exhibit the highest actual specific capacity when the molar ratio of PPD to BQ is 1:1. In addition, comparison among PPD-BQ/RGO-B-1, -4, -5, and -6 demonstrates that the composite films achieve the best electrochemical performance when the feed ratio of PPD:BQ:GO is 1:1:3. Therefore, the synthesis conditions used for PPD-BQ/RGO-B-4 were selected as optimal.

As shown in Figure S4c, comparison among PPD-BQ/RGO-C-1, -2, and -3 reveals that the composite films exhibit the highest specific capacity and cycling stability at a reaction temperature of 65 °C. At lower temperatures, the polymerization reaction proceeds more slowly, leading to insufficient polymer growth on the GO surface. In contrast, excessively high temperatures may weaken the interfacial association between the polymer and GO nanosheets, which is unfavorable for the in situ growth process. Therefore, 65 °C was selected as the optimal reaction temperature.

As shown in Figure S4d, comparison among PPD-BQ/RGO-D-1, -2, -3, and -4 shows that the composite films exhibit the best electrochemical performance at a reaction time of 24 h. Short reaction times result in insufficient polymer loading on the GO nanosheets, whereas excessively long reaction times lead to excessive polymer deposition, which decreases the conductivity of the composite films and limits the utilization of active materials. Therefore, 24 h was selected as the optimal reaction time.

In summary, 20 mg of PPD, 20 mg of BQ, 20 g of GO aqueous dispersion (3 mg g−1), and 5 mL of hydrochloric acid (37%) were sequentially added into a three-necked flask and reacted at 65 °C for 24 h in an oil bath. After subsequent reduction with hydrazine hydrate and vacuum filtration, the optimized composite films, denoted as PPD-BQ/RGO, were successfully obtained.

Figure S5 SEM image of RGO.

Figure S6 BET analysis of PPD-BQ/RGO composite films: (a) N₂ adsorption–desorption isotherms and (b) pore-size distribution.

Figure S7 XRD patterns of PPD-BQ, RGO, and PPD-BQ/RGO composite films.

Figure S8 CV curves of PPD-BQ/RGO composite films at scan rates of 0.5, 1, 2, 5, and 10 mV s−1.

Figure S9 Electrochemical performances of PPD-BQ/RGO composite films within different voltage windows.

Figure S10 Galvanostatic charge–discharge curves of pure RGO electrodes.